	PSGSG/12-13/02
	SPECIFICATIONS FOR

“O RINGS”
	Drg.No.
	

	
	
	Date 
	18.06.14

	
	
	
	

	
	
	Product
	GSM145

	1.0


	APPLICATION:

EPDM “O rings” as per dimensions given below are required for sealing gas insulated switchgear equipment.


	2.0

2.1

2.2
	SPECIFICATION:

Material  :          EPDM
“O-rings” as per following profile with S.H. of 70 ± 5 have to be supplied:

[image: image1]


	Page

1/2
	PSGSG/12-13/02.doc 
	
	Signature









           Contd..

	PSGSG/12-13/02
	SPECIFICATIONS FOR

“O RINGS”
	Drg.No.
	

	
	
	Date 
	18.08.14

	
	
	
	

	
	
	Product
	GSM145

	2.3

2.4
2.5
2.6
2.7
2.8
	List of “O Rings” to be supplied:

S.No

Inner Diameter (ID), mm

Thickness in (mm)
Qty.
1

265
8
150

2
265
7.5
 150
The supplier shall submit material composition report and 
hardness values for the material. 

The component shall be free from pin holes, cracks 
and shall be leak proof. Necessary test reports shall
 be furnished. O-rings shall be part of switchgear 
equipment which works under the gas pressure difference 
of 11.0 bar.
The supplier shall quote on the basis of per unit of each
 type of O-ring.
The material shall be packed individually in appropriate
 packing so as to protect o-ring surface and prevent 
de-shaping of the material during transportation.

Test certificates shall be provided along with the delivery of the components.



	 Page

 2/2
	PSGSG/12-13/02.doc 
	       Signature




� EMBED AutoCAD.Drawing.17  ���








4
2

[image: image2.wmf]_1252498128.dwg

