	PSGSG/12-13/06
	Product Specifications

For

NYLOCAST RODS  
	Drg. No.
	

	
	
	Date
	15.05.14

	
	
	Product
	GSM420

	   1.0

2.0

3.0
4.0

   5.0

	 Application                          :   SWITCHGEAR
 Configuration                      :  Nylocast rods shall be as per dimensions.
 Color                                    :  Natural  colour of Nylocast
Quantity                              :  6 No.s
Specifications:

1. Dimensions                       : Dia 300.0mm x 180.0mm                 
2. Material                          :  Nylocast
3. Properties :
      Compressive Strength  (kgf/cm2)   : 1200

     Specific gravity  (gm/cc)                :1.15

     Hardness                                     :  78-86
    Tensile strength at yield  (kgf/cm2  :   ~850 
     Service Temperature (max)           :90-130 C

 

	1/2
	PSGSG/12-13/06.doc


	
	Signature



	PSGSG/12-13/06
	Product Specifications

For

NYLOCAST RODS
	Drg. No.
	

	
	
	Date
	15.05.14

	
	
	Product
	GSM420

	6.0

   7.0

8.0


	Tests:

(a). Dimensional : All dimensions shall as per specifications.

(b). Material Certificate shall be submitted along with the supply. 

Packing : 

The nylocast rods shall be packed in high density cardboard boxes, with a primary wrapped in polyethylene and packed individually in dust free boxes after degreasing. The component shall be guaranteed against all material and manufacturing defects for at least one year.

General :

1. Surface finish of the components shall be at least RA 1.6.

2. The component shall be free from dirt, grease and loose particles.

In case of doubts in drawings or specifications the supplier shall contact BHEL for clarifications.

	2/2
	PSGSG/12-13/06.doc


	
	Signature




