	PSGSG/12-13/03
	Product Specifications

For

ALUMINIUM TUBES
	Drg. No.
	

	
	
	Date
	5.07.14

	
	
	Product
	GSM 400

	1.0

2.0

3.0

4.0


	 Application:      

Aluminum tubes shall be used for Gas Insulated switchgear Equipment     

 Material: HE -30 Aluminum tubes

Dimensions: 
S.No

Inner Diameter (ID), mm

Outer Diameter (OD), mm
Length(mm)
Qty.
1

100±0.5
320 ±0.5
60±1
10
2
180±0.5
325±0.5
450±1
4
Specifications:

1.Electrical conductivity of material shall be greater than 45

   %. (IACS)

2. Surface finish of the components shall be at least RA 0.8.

3. The component shall be free from dirt, grease and loose

 particles.



	1/2
	PSGSG/12-13/03.doc


	
	Signature




