	PSGSG / 11-12/05
	Product Specifications

For

High Electrical Conductivity Copper rods
	Drg. No.
	

	
	
	Date
	05.07.2014

	
	
	Product
	GIS

	  1.0

2.0

3.0

4.0

4.1
4.2
4.3
5.0
6.0

	 Application                                           : High voltage Switchgear
 Material                                               : High conductivity Electrical Grade (ETP grade)  

                                                             copper rods
Quantity                                                : 1)8 No. s of  following sample 
100±0.5mm DIA x 120±2  mm Long
                                                              2)6No. s of  following sample 

170±0.5mm DIA x 70±2  mm Long

Specifications:

The specified copper material shall have minimum conductivity of 95 % IACS. Supplied 

material will be tested at BHEL for conductivity and the same will be rejected in case they 

do not meet specified conductivity.

The material shall be good for brazing, soldering and for electrical applications where high 

Current transfer in involved.
Quotation shall be submitted by supplier on price per piece basis only.

Dimensional check 

The material shall comply to specified sizes.
Packing : 

The copper rods shall be packed in dust free boxes.
General:
 The components shall be guaranteed against all manufacturing defects.

	1/1
	PSGSG /11-12/05
	
	Signature


